Technical Data Sheet (Version 4 : June 2017)

SENSOCRYL AS 60 LIQUID

| PRODUCT Sensocryl AS 60 Liquid is a crosslinked acrylic emulsion copolymer for thickening water based paints and coatings |  |
| --- | --- |
| USE Sensocryl AS 60 Liquid is recommended for paint industry |  |
| DIRECTION FOR USE Mixing : The drum should be rolled if stored for long time |  |
| DESCRIPTION Sensocryl AS 60 Liquid is Styrene acrylic copolymer dispersion |  |
| ASPECT | White liquid |
| COLOR | Milky |
| SPECIFIC GRAVITY (GM/CC) | 1.057 ± 0.1 |
| pH , 10% | 4.5 ± 0.1 |
| VISCOSITY , CPS , 25 DEG. |  |
| SOLID CONTENT@ 110°C,2 hrs | 28.00 % ± 1.0 % |
| IONIC NATURE | Anionic |
| Tg (Deg.c) |  |
| ADVANTAGES | - Ease of application - Used for thickening latex for floc applications - Useful in viscosity adjustment of emulsion and latex compounds of many types - Highly efficient thickener with good stability Used to suspend pigments and fillers in water-based paints, inks or other coatings and the abrasive particles in waxes or polishes |
| PRECAUTION Sensocryl AS 60 Liquid should be applied on dry tile surface. For achieving best result it is advisable to polish the surface continuously by mechanical grinding. |  |
| DOSAGE For any query please contact your local Rossari representative . |  |
| PERFORMANCE Sensocryl AS 60 Liquid should not be diluted with water or mixed with any other chemical because it hampers the performance. |  |
| CLEANING Sensocryl AS 60 Liquid should be removed from tools, equipment and mixers with clean water immediately after use. Hardened material can only be removed mechanically. |  |
| LIMITATIONS Sensocryl AS 60 Liquid should not be used when the temperature is below 5 degrees C and falling. |  |
| PACKAGING Sensocryl AS 60 Liquid is available in 220 kg HDPE drum |  |
| SHELF LIFE Sensocryl AS 60 Liquid has a shelf life of 6 months if kept in a dry store in the original, unopened drum. If stored at high temperature and / or high humidity conditions the shelf life may be reduced. |  |
| SAFETY Avoid direct contact of Sensocryl AS 60 Liquid with skin and eyes. Wear suitable protective clothing, eye protection, gloves and respiratory equipment (particularly in confined spaces). The use barrier creams to provide additional skin protection. In case of contact with the skin, rinse with plenty of clean water, then cleanse thoroughly with soap and water. In case of contact with eyes, rinse immediately with plenty of clean water and seek medical advice. If swallowed seek medical attention immediately - do not induce vomiting. Sensocryl AS 60 Liquid is water based and so it is not flammable. For more detail safety and environmental guidance please consult material safety data sheet |  |
| Special Note The aforementioned data is the agreed quality of the product at the time of production and checking the quality during approval. The data are controlled at regular intervals as part of our quality assurance program. Neither these data nor the properties of product specimens shall imply any legal binding of certain properties or of fitness for a specific purpose. It is user's responsibility to check the substrate and compatibility or suitability of the product for deemed application. |  |